## Slide 1
产品尺寸Produce Size: 185X81X53mm
项目名称:

## Slide 2
产品/模具分析：Product/Mould Structure Analysis
日期 Date:
Product Name:
Machine Type:160t
模具编号： No:
Cavity:1*1
Shrinkage: 1.015
Surface Treatment :
Part Material：pp
Core Material: 718h
Surface: texture
Cavity Material: 718h
Runner Type: hot Runner
Mould Type: Injection Mould
Mould Base Material:1.1730
Slider Material: 718h
客户产品编号：Product No:
Actual Clamping :
Mould Structure : 2 Plate

## Slide 3
拔模分析:
Demoulding Analysis
The blue surface has no inclination and needs to be modified

## Slide 4
壁厚分析:
Part Thickness Analysis
The red surface is thicker, and there will have sink marks

## Slide 5
The bule line is part line, the arrow is demoulding direction
型芯
Core side
型腔
Cavity side
分型线:
Part Line

## Slide 6
模具结构：
Mould Structure
2lifter

## Slide 7
模具尺寸：
Mould Size
Mould Size: 380X280X480mm

## Slide 8
浇口位置：
Gate Position
浇口类型gate：一点热流道，点浇口 1 point gate hot runner

## Slide 9
顶针位置和冷却水路：
Ejector Position on Core and Cooling System

## Slide 10
Before modification
After modification
Boss posts need to be modified; otherwise, sink marks will easily occur.

## Slide 11
Ribs are too thick and prone to sink marks. Suggest thickness down to around 1mm.

## Slide 12
PP deforms easily and cannot meet tolerances. Recommend ABS plus extra positioning for assembled parts.
Strong rigidity, little distortion.
Weak strength, heavy distortion.

## Slide 13
Before modification
After modification
Clips are not strong enough, please revise.

## Slide 14
Thank you!
END